# TERRY

(All Sizes in CM)

|  | BATH TOWEL | HAND TOWEL | WASH CLOTH | BATH MAT |
| --- | --- | --- | --- | --- |
| FINISHED SIZE AFTER SHRINKAGE | 74 X 150 | 50 X 100 | 30 X 30 | 50 X 90 |
| WEIGHT GSM PRIOR TO LAUNDERING | 570gsm | 570gsm | 500gsm | 800gsm |
| BLEND | 100% Cotton | 100% Cotton | 100% Cotton | 100% cotton |
| LOOP YARN SIZE | 22/1 Combed Ring Spun | 22/1 Combed Ring Spun | 22/1 Combed Ring Spun | 12/1Combed Ring Spun |
| HEM STITCHES/CM | 3 | 3 | 3 | 3 |
| HEM | Lock stitched, bar tacked hem | Lock stitched, bar tacked hem | Lock stitched, bar tacked hem | Lock stitched, bar tacked hem |
| BORDER TYPE | None | None | None | None |
| BORDER WIDTH | 7.6cm | 5cm | n/a | n/a |